## Slide 1
Molecular Simulations of
Metal-Organic Frameworks
Jeffery A. Greathouse
Sandia National Laboratories
9 August 2011
Sandia National Laboratories is a multi-program laboratory managed and operated by Sandia Corporation, a wholly owned subsidiary of Lockheed Martin Corporation, for the U.S. Department of Energy’s National Nuclear Security Administration under contract DE-AC04-94AL85000.

## Slide 2: Outline
Metal-organic frameworks (MOFs)
MD simulation
  Mechanical properties
  Vibrational properties
  Framework stability
GCMC simulation
  Code development (Paul Crozier)
  Adsorption of I2 by ZIF-8
IRMOF-1

## Slide 3: Metal-Organic Frameworks (MOFs)
nbo
NOTT-10x, PCN-14
Cu2 cluster
sod
ZIF-8
Zn cluster
seh
MIL-53(Al)
Al(OH) cluster
pcu
IRMOF series
Zn4O cluster
Crystalline, highly ordered solids
Metal cations linked by organic linkers
Tunable pore chemistry
Nanoporous (5-30 Å)
Huge variety of structures
Ultrahigh surface areas
    (as high as 6000 m2/g)
Structurally flexible

## Slide 4: MD Simulation
Potential energy expression:
  All atoms: VDW and electrostatic
  Linkers and adsorbates: CVFF intramolecular parameters (bond, angle, dihedral, out-of-plane
Constant pressure (NPT) ensemble to calculate volume and lattice parameters (with and without adsorbate).
Constant volume (NVT) ensemble for elastic and vibrational properties.
Nonbonded force field approach for IRMOF-1 validated by: T and P effects, elastic properties, vibrational properties, volume changes associated with adsorption (water)

## Slide 5: Mechanical Properties of IRMOF-1
Greathouse and Allendorf, J. Phys. Chem. C 2008.
 | Energy Min (0 K) |  | MD Sim (300 K)
 | FF | DFT | FF
Bulk Modulus (GPa) | 20.0 | 16.3 | 4.0
Trend of negative thermal expansion agrees with experiment.
1.0% increase in volume between 30 K – 293 K (0.1 Å in lattice parameter).
Significant decrease in bulk modulus between 0 K and 300 K

## Slide 6: Vibrational Properties of IRMOF-1
Greathouse and Allendorf, J. Phys. Chem. C 2008.
Librational modes due to internal rotation of phenyl groups.
Power spectra for select atom types. Frequencies for ZnO4 modes are in agreement with experiment.

## Slide 7: Interaction of IRMOF-1 with Water
Greathouse and Allendorf, J. Am. Chem. Soc 2006.
Framework unstable at higher water content
Framework distortion at low water content

## Slide 8: Adsorption in LAMMPS: “fix GCMC”
Grand canonical Monte Carlo (VT ensemble)
Standard GCMC features:
  Particle creation/destruction.
  Work efficiently, and in parallel on multiple processors.
  Compatible with other LAMMPS features (MD, ensembles, force fields, computes, etc).
  Reports relevant statistics.
Currently limited to monatomic adsorbates and short-range interactions (no electrostatics).

## Slide 9: Adsorption of I2 in ZIF-8
Spherical model for I2.
Predicted I2 loading in good agreement with x-ray diffraction.
Sava et al, J. Am. Chem. Soc. 2011, in press.

## Slide 10: More on “fix GCMC”
Likely to be done soon:
More verification testing vs MCCCS Towhee code.
Fix code problems identified by beta testers.
Improve the documentation in preparation for release.
Send updated code & docs out to beta testers and Steve.
Release code & docs on main LAMMPS website.
Maybe later if there’s time:
Add molecule capability, including MC exchanges, moves, and rotations of molecules.
Add ability to measure and report chemical potential.
Make it work with long-range electrostatics.
Make it scale: better parallel simulation.
Add fancier MC moves (configurational bias, etc.).

## Slide 11: Acknowledgements
Sandia National Laboratories
  Mark Allendorf
  Paul Crozier
  Tina Nenoff
  Dorina Sava