## Slide 1: Charge Optimized Many Body (COMB) Potential in LAMMPS
Ray Shan, Simon R. Phillpot, Susan B. Sinnott
Department of Materials Science and Engineering
University of Florida
LAMMPS Users’ Workshop
August 9th 2011
Supported by: NSF-DMR, DOE EFRC, NSF-CHE, DOE
Notes: Good afternoon, ladies and gentlemen. I am Ray Shan, from the University of Florida and I work with Profs. Simon Phillpot and Susan Sinnott. My talk for the next 15 minutes is to introduce a recently implemented pair style: the Charge optimized many body potential. Before I start, I would like to acknowledge Steve and Aidan for their kind assistance when we were implementing the potential into LAMMPS.

## Slide 2: Outline
Introduction to the COMB potentials
Comparisons to other empirical potentials
Applications of the COMB potentials
  Adhesion of Cu/SiO2 interfaces
  Nanoindentation and nanoscratch of Si/a-HfO2
  Modeling Cu/Cu2O interface
  C/H/O and Zr/ZrO2 potential development
  Cu ad-atom on ZnO surface via adaptive kinetic Monte Carlo
Conclusions
Notes: This is a brief outline of my talk. I will start with an introduction to the COMB potential, and then provide a comparison of COMB to other potentials that are available in LAMMPS with some examples. Then I will go through several applications with the COMB potentials

## Slide 3: Visual presentation of COMB potentials
Metallic
Ionic
Covalent
Bone/biocomposites
Aqueous biological systems
Interconnects
Corrosion/Oxidation
Thermal barrier coatings
Catalysts
S. R. Phillpot, S. B. Sinnott, Science 325, 1634 (2009).
Cu, Al, Hf, Ti, Zr, U, Zn
Si, C/H/O/N
SiO2, Cu2O, Al2O3,
HfO2, TiO2, ZrO2,
UO2, ZnO, AlN, TiN
Notes: This figure visually presents the capabilities of COMB. COMB is a variable charge empirical potential that is designed to model nanostructures composed of heterogeneous interfaces. Such interfaces consist of discrete bonding types and it has been a challenge to model these interfaces with empirical potentials. For example, catalysts includes interfaces between covalent and metallic bonding types, interconnects include metallic and ionic bonds, and microelectronic devices are composed of all three types of bonding types.

## Slide 4: Functional form of COMB potential
General formalism:
  Self energy: fit to atomic ionization energies and electron affinities
  Interatomic potential: Charge dependent Tersoff + Coulomb
  Spherical charge distribution: 1s-type Slater orbital
  1 J. Yu, et. al., Phys. Rev. B 75 085311 (2007)
2 T.-R. Shan, et al., Phys. Rev. B 81, 125328 (2010)
Notes: Self energy, which is a fourth order polynomial, is fit to ..
… in the COMB formalism, charges are treated as spherical charge densities centered around each atom, for which we use 1s-type Slater orbital to describe the charge densities.

## Slide 5: Overview of COMB potentials
1st generation a
  Si/SiO2, Cu
  Tersoff + Coulomb (point charge model with cutoff) + QEq
  In-house HELL code
2nd generation b
  Si/SiO2, Cu/Cu2O, Hf/HfO2, Ti/TiO2
  Tersoff + Coulomb (spherical charge density with Wolf Sum) + Qeq
  In-house HELL code, implemented into LAMMPS
3rd generation c
  C/H/O/N, Zr/ZrO2, Zn/ZnO, U/UO2, Al/AlN/Al2O3, Ti/TiN/TiO2
  Improved bond-order term
  Implementation into LAMMPS undergoing
  a J. Yu, et. al., Phys. Rev. B 75 085311 (2007)
b T.-R. Shan, et al., Phys. Rev. B 81, 125328 (2010)
c T. Liang, et al., in preparation

## Slide 6: Use COMB potentials in LAMMPS
2nd Generation COMB
  atom_style charge
  pair_style comb
  pair_coeff * * ffield.comb Si O Cu
  fix ID group-ID qeq/comb 1 1e-4 file fq.out
3rd Generation COMB
  atom_style charge
  pair_style comb3
  pair_coeff * * ffield.comb3 Cu C H O
  fix ID group-ID qeq/comb 1 1e-4 file fq.out
Notes: To use COMB in LAMMPS, first you have to enable the manybody package since it is implemented as a pair style.

## Slide 7: Variable Charge Equilibration
Electronegativity equalization principle
Extended Lagrangian method
  Si-NC
  a-SiO2

## Slide 8: Outline
Introduction to the COMB potential
Comparisons to other empirical potentials
Applications of the developed potentials
  Adhesion of Cu/SiO2 interfaces
  Nanoindentation and nanoscratch of Si/a-HfO2
  Modeling Cu/Cu2O interface
  C/H/O and Zr/ZrO2 potential development
  Cu ad-atom on ZnO surface via adaptive kinetic Monte Carlo
Conclusions

## Slide 9: Cost of Potentials in LAMMPS
Potential | System | # Atoms | Memory | LJ Ratio
Lennard-Jones | LJ liquid | 32000 | 12 Mb | 1.0x
EAM | bulk Cu | 32000 | 13 Mb | 2.4x
Tersoff | bulk Si | 32000 | 9.2 Mb | 4.1x
Stillinger-Weber | bulk Si | 32000 | 11 Mb | 4.1x
EIM | crystalline NaCl | 32000 | 14 Mb | 6.5x
CHARMM + PPPM | solvated protein | 32000 | 124 Mb | 13.6x
MEAM | bulk Ni | 32000 | 54 Mb | 15.6x
AIREBO | polyethylene | 32640 | 101 Mb | 54.7x
ReaxFF/C | PETN crystal | 32480 | 976 Mb | 185x
COMB2 (fixed q) QEq | Ti crystalline SiO2 | 32400 32400 | 31 Mb 85 Mb | 55x 284x
eFF | H plasma | 32000 | 365 Mb | 306x
ReaxFF | PETN crystal | 16240 | 425 Mb | 337x
VASP/small | water | 192 (512e-) | 320 procs | 17.7×106
http://lammps.sandia.gov/bench.html

## Slide 10: Modeling C2H4 molecule
 | REBO * | AIREBO | ReaxFF/C | COMB fix | COMB qeq
Energy of C2H4 (eV/atom) | -4.05 | -4.05 | -106.92 | -3.83 | -3.88
Relative energy, △E (eV/atom) | + 0.69 | + 0.7 | + 7.51 | + 0.65 | + 0.7
CPU time (sec/105 step) | 3.7 | 10.0 | 43.5 | 7.2 | 35.3
Charge on C | -- | -- | -0.11 | 0.0 | -0.15
REBO, AIREBO, ReaxFF and COMB capable of modeling torsionals
COMB and ReaxFF capable of variable charges
C2H4
C2H4p
△E from QC: 0.75 eV/atom
* With in-house serial REBO code

## Slide 11: Modeling Cu crystal
Scaling of COMB and EAM in LAMMPS
  System sizes vary from 500 to 64,000 atoms
  8 CPUs, Intel Xeon 2.27 GHz
  COMB costs ~25 times more than EAM
Chart: log (Number of atoms)
| 500.0 | 4000.0 | 13500.0 | 32000.0 | 62500.0
COMB | 31.645 | 162.403 | 536.631 | 1281.01 | 2506.91
EAM | 2.4853 | 7.4961 | 13.52 | 53.208 | 80.8428
 | EAM 1 | COMB 2
a0 (Å) | 3.615 | 3.615
Ecoh (eV) | -3.54 | -3.51
C11 (Gpa) | 170 | 169
C12 (Gpa) | 123 | 119
C44 (Gpa) | 76 | 52
MD Time (seconds． 103 atom-1．103 steps-1) | 2.1 | 44.8
1 Y. Mishin, JM Mehl, DA Papaconstantopoulos, AF Voter, JD Kress, Phys. Rev. B 63, 224106 (2001).
2 J Yu, SR Phillpot, SB Sinnott, Phys. Rev. B 75, 233203 (2007).

## Slide 12: Outline
Introduction to the COMB potential
Comparisons to other empirical potentials
Applications of the developed potentials
  Adhesion of Cu/SiO2 interfaces
  Nanoindentation and nanoscratch of Si/a-HfO2
  Modeling Cu/Cu2O interface
  C/H/O, Zr/ZrO2 and U/UO2 potential development
  Cu ad-atom on ZnO surface via adaptive kinetic Monte Carlo
Conclusions

## Slide 13: Cu (001)/a-SiO2 Interfaces
Structural properties of the interface
  Oxidation of Cu is limited to the first two Cu layers; formation of Cu2O
Type of interface | W (J/m2) |  | Cu-O (%)
 | Exp | COMB | 
Cu/a-SiO2 + 0 VO | 0.5 - 1.2 b 0.6 - 1.4 c | 1.810 | 22
Cu/a-SiO2 + 10 VO |  | 0.629 | 13
Cu/a-SiO2 + 20 VO |  | 0.289 | 11
a T.-R. Shan, B. D. Devine, S. R. Phillpot, and S. B. Sinnott, Phys. Rev. B 83 115327 (2011).
b T. S. Oh, R. M. Cannon, and R. O. Ritchie, J. Am. Ceram. Soc. 70, C352 (1987).
c M. Z. Pang and S. P. Baker, J. Mater. Res. 20, 2420 (2005).
  Cu-O bonds play crucial roles in adhesion of the interface
Adhesion of Cu/dielectric layer decreases with O defects
Introduced O vacancies at the interface
  0, 10 and 20 VO

## Slide 14: Cu(100) [001]∥Cu2O(111)[112] Interface
Electrochemically deposited Cu2O film grows in (111) direction on Cu(100)
  Atomically sharp, semi-coherent
Modelled with COMB potential
  Coherent, 3.6% lattice mismatch
  Negligible charge transfer between phases
  No unphysical charge leaks
  May be applied to study Cu2O growth on Cu surfaces
B. D. Devine, T.-R. Shan, Y.-T. Cheng, M.-Y. Lee, A. J. McGaughey, S. R. Phillpot, and S. B. Sinnott, Phys. Rev. B, in press
Interface adhesion strength:
DFT: 1.96 J/m2
COMB: 2.77 J/m2

## Slide 15: Nanoindentation of Si/a-SiO2
Snapshot of the system
Simulation set ups
  Rigid Si indenter, 1 m/s indentation rate at 300K
  Movie: 10 ps/frame, 2 ns MD time
Interface stronger and stiffer with variable charge
Load-displacement curves
1.2 nm
T.-R. Shan, X. Sun, S. R. Phillpot, and S. B. Sinnott, in preparation

## Slide 16: Modeling Polycrystalline Zr with COMB
On-going mechanical testing on polycrystalline Zr metal
  2D columnar grains, 17 nm in diameter
Color coded by coordination,
courtesy of Dong-Hyun Kim and Zizhe Lu

## Slide 17: COMB Potentials for CHO Systems
CH3CHO (acetaldehyde)
Development ongoing, considering more CH and CHO molecules
Combining with COMB potentials for metals and oxides
  Able to model complex organic/inorganic systems
B3LYP COMB
En (eV) -4.14 -4.26
qC1 (e) -0.68 -0.56
qC2 (e) 0.12 -0.01
qO1 (e) -0.27 -0.21
R1 (Å) 1.09 1.15
R2 (Å) 1.51 1.49
R3 (Å) 1.20 1.17
R1
R2
R3
C1
C2
O1
T. Liang, et al., in preparation

## Slide 18
Charge of Cu cluster on ZnO(10-10) predicted by COMB
Diameter: ~ 15 Å
Height: ~ 6 Å
STM image of Cu clusters on
ZnO(10-10) surface
0.4587
-0.4581
Charge Transfer at Cu/ZnO Interfaces as Predicted by the COMB Potential
Courtesy of Yu-Ting Cheng

## Slide 19
Adaptive Kinetic Monte Carlo
Ea
Pathway for single Cu atom diffusion on Cu(100) from the aKMC calculations
0.88
0
(eV)
(displacement)
 | Activation energy (eV)
COMB | 0.88
Adaptive KMC | 0.88
Courtesy of Yu-Ting Cheng

## Slide 20: Conclusions
An empirical, variable charge many body (COMB) potential developed for modeling heterogeneous interfaces
  COMB2 Parameterized for Si/SiO2, Cu/Cu2O, Hf/HfO2 and Ti/TiO2
  COMB3 being developed for C/H/O/N, Zr/ZrO2, Zn/ZnO, U/UO2, Al/Al2O3, Ti/TiN/TiO2
  Implemented in community popular MD software LAMMPS
Enables large scale MD simulations of complex, real device-size multifunctional nanostructures with technological significance
Modified formalism with improved flexibility is currently being parameterized for more systems