## Slide 1
Molecular Dynamics Simulations of Radiation Damage in Amorphous Silica:
Effects of Hyperthermal Atomic Oxygen
Vanessa Oklejas
Space Materials Laboratory
The Aerospace Corporation
Motivation
Neutral atomic oxygen is the dominant species in low earth orbit (LEO).
Spacecraft materials undergo significant erosion due to atomic oxygen in LEO; the mitigation of radiation damage of spacecraft materials is a major concern.
Use MD simulations to understand how radiation modifies the molecular and mechanical properties of materials.
© 2013 The Aerospace Corporation
This work was supported under The Aerospace Corporation's Independent Research and Development Program.
Results
Conclusions & Future Work
  Significant displacement damage was observed for simulations of AO projectile atoms with 100 eV energies, which was accompanied by changes in ring structure.
Limited damage was also observed for AO projectiles with energies below those typically used to model displacement damage (i.e., the threshold displacement damage, Ed).
Simulate and identify the formation of stable silica defects due to radiation-induced damage.
Examine radiation-induced changes in the material at the atomic level
Radiation-induced chemical changes
High energy AO projectiles introduce chemical changes in the silica model that, over time, will develop into stable defects. Defects are associated with performance degradation of amorphous silica (e.g., darkening, development of charge traps, decrease in mechanical strength).
Averaged Displacement Damage
An increase in the larger ring sizes and a loss of most stable ring sizes was observed.
Methods
A reactive force field (ReaxFF) was used to represent inter-atomic interactions.1
  Preparation of amorphous silica substrate:
  A simulation box of 2000 SiO2 moieties was heated to 4000 K and cooled at a rate of ~ 1013 K/sec. ( = 0.25 fs)
  The first annealing cycle was performed using the NVT ensemble followed by a final annealing cycle in the NPT ensemble.
  A free surface was generated at the xy- plane.
Radiation Simulations
MD simulation parameters:
  NVE ensemble;  = 0.125 fs.
  Oxygen atom placed 5 Å above silica surface.
  Total simulation time was 32 ps.
Image details:
  AO shown as red sphere.
  Displaced atoms shown as pink (O) or cyan (Si) spheres.
  Original positions of atoms are rendered transparent.
  Silicate network shown as transparent sticks.
Silica tetrahedrons are connected to one another by bridging O atoms
12 node ring
Silicate ring structure describes connectivity in amorphous silicate materials.2
Larger rings are associated with nanoscale void formation.
Molecular dynamics simulations were used to investigate the damage created in amorphous silica by hyperthermal atomic oxygen (AO) as a function of incident kinetic energy.
100 eV
4 eV
30 eV
Small amount of displacement damage observed for AO with energies below Ed .
AO Penetration Depth
surface
100 eV
Penetration depth is commensurate with displacement damage.
4 eV
30 eV
Radiation-induced changes in silicate ring structure
100 eV
4 eV
30 eV
References
Fogarty, J.C.; Aktulga, H.M.; Grama, A.Y.; van Duin, A.C.T.; Pandit, S.A., J. Chem. Phys., 132, 174704 (2010).
Le Roux, S.; Jund, P., Comp. Mater. Sci., 49, 70-83 (2010).
Amorphous Silica Model
α-quartz
amorphous silica